Geochemistry and S, Pb isotope of the Yangla copper deposit, western Yunnan, China: Implication for ore genesis

Xi-An Yang a, Jia-Jun Liu a﹡, Ye Cao a, Si-Yu Han a, Bing-yu Gaoa, Huan Wang a , Yue-Dong Liu b

a State Key Laboratory of Geological Process and Mineral Resources, China University of Geosciences , Beijing 100083, China

b Yunnan Diqing Mining Industry Group, Deqin 674507, China

ABSTRACT: The Yangla copper deposit, situated in the middle section of Jinshajiang tectonic belt between Zhongza-Zhongdian block and Changdu-Simao block, is a representative and giant copper deposit that has been discovered in Jinshajiang-Lancangjiang-Nujiang region in recent years. There are coupled relationship between Yangla granodiorite and copper mineralization in the Yangla copper deposit. Five molybdenite samples yielded a well-constrained 187Re-187Os isochron age of 233.3±3 Ma, the metallogenesis is therefore slightly younger than the crystallization age of the granodiorite. S, Pb isotopic compositions of the Yangla copper deposit indicate that the ore-forming materials were derived from the mixture of upper crust and mantle, also with the magmatic contributions. In the late Early Permian, the Jinshajiang Oceanic plate was subducted to the west, resulting in the formation of a series of gently dipping thrust faults in the Jinshajiang tectonic belt，meanwhile, accompanied magmatic activities. In the early Late Triassic, which was a time of transition from collision-related compression to extension in the Jinshajiang tectonic belt, the thrust faults were tensional; it would have been a favorable environment for forming ore fluids. The ascending magma provided a channel for the ore-forming fluid from the mantle wedge. After the magma arrived at the base of the early-stage Yangla granodiorite, the platy granodiorite at the base of the body would have shielded the late-stage magma from the fluid. The magma would have cooled slowly, and some of the ore-forming fluid in the magma would have entered the gently dipping thrust faults near the Yangla granodiorite, resulting in mineralization.

Key words: Western Yunnan; Yangla copper deposit; Geochemistry；S, Pb isotope

﹡Corresponding author at: State Key Laboratory of Geological Process and Mineral Resources, China University of Geosciences, 29 Xueyuan Road, Beijing 10083, China.

E-mail address: liujiajun@cugb.edu.cn (J.J. Liu)

- Introduction

The Yangla copper deposit is located in the Yangla area of the Henduan Mountains in Deqin County, Yunnan Province, southern Tibet. A team from the Yunnan Geology and Exploration Bureau discovered the deposit in 1965 in the course of mapping and exploring the area, mining of the Yangla copper deposit started in November 2007. The deposit was investigated by the third Regional Geological Survey Team of Sichuan Province, the third Team of Yunnan Geology and Exploration Bureau, the China University of Geosciences, the Yichang Institute of Geology and Mineral Resources, and the Chengdu Institute of Geology and Mineral Resources, among others (Qu et al., 2004). The deposit has copper reserves of 1.2 Mt (Yang, 2009), and given its location in the Jinshajiang tectonic zone (Pan et al., 2001), this region has great potential for further exploration. Previous studies have reported the structural characteristics (Lin and Wang, 2004), geochemical characteristics of the ores and the rocks in the Yangla copper deposit (Wei et al., 1997; Pan et al., 2000), however, the ore genesis of the deposit is still debated. Wei et al. (1999) suggested that the deposit is a VMS type, a conclusion later supported by Pan et al. (2003). Based on geochemical evidence of ore-bearing skarns, Lu et al. (1999) and Wei et al. (2000) concluded that the deposit is a skarn-type deposit related to the Yangla granodiorite. Lin et al. (2004), Hu et al. (2008), Li et al. (2008) and Liu et al. (2009) suggested that the deposit is structurally controlled.

Recent mining exposures at the Yangla copper deposit provided an ideal opportunity for detail underground investigation and systematic sampling. In this paper, we present a comparison of the REE and trace element compositions of the ores with those of the Yangla granodiorite, S, Pb isotopic composition, and molybdenite Re–Os isotopic dating of the Yangla copper deposit. We discuss the origin of ore-forming materials and the ore genesis of the Yangla copper deposit. The results contribute to our understanding of the genesis of the Yangla copper deposit and will guide further exploration in the region.

2.  Economic geology of the Yangla copper deposit

The Jinshajiang–Lancangjiang–Nujiang region in southwestern China is located in the eastern part of the Tethyan–Himalayan tectonic belt, and also in the tectonic junction between Gondwanaland and Eurasia (Hou et al., 2003). Several of the Paleozoic sutures in the region provide a record of the history of the Paleo-Tethys Ocean, which consists of four paleooceanic basins: the Ganzi–Litang, Jinshajiang, Lancangjiang and Changning–Menglian oceans from east to west (Jian et al., 2009). The birth and final closure of the Paleo-Tethys Ocean are associated with the breakup and assembly of Gondwanaland (Xiao et al., 2008). It has been commonly accepted that the Changning-Menglian Suture Zone is the main boundary that separates the Yangtze Block from Gondwanaland (Jian et al., 2009), and that the Changdu-Simao and Zhongza micro-continental Blocks were marginal terranes of the Yangtze Block (Wang et al., 2000; Metcalfe, 2002; Zhu et al., 2011).

The Yangla copper deposit is located in the middle part of the Jinshajiang tectonic belt (Fig. 1). The Jinshajiang tectonic belt, regionally situated between Zhongza block to the east and Changdu-Simao block to the west, which developed in the late Paleozoic due to subduction of the Jinshajiang Oceanic block, and has experienced multiple tectonic processes (e.g., rifting, extension, subduction, and continent–continent collision) during the latest Permian to latest Middle Triassic.

2.1. Stratigraphy

The Jinshajiang tectonic belt has been subjected to intense compression during the geological evolution of the Jinshajiang–Lancangjiang–Nujiang region; consequently, the rocks are fragmented and faults are widely developed. No stratigraphy is preserved: the various rock types occur as fragments (Feng et al., 1999) that show no common stratigraphy, occurring instead as mélange (Qu et al., 2004). Previous studies proposed various stratigraphic schemes for the Yangla area (He et al., 1998; Qu et al., 2004; Zhu et al., 2009). Surface rocks are dominated by the Gajinxueshan Group, which is a suite of sediments, including quartz schist, biotite plagioclase gneiss, metasandstone, quartzite, marble, slate, volcanoclastics, and andesite, with ages ranging from the Neoproterozoic to the Carboniferous. The ore deposit at Yangla is hosted in the Devonian Jiangbian suite (marble interlayered with sericite quartz schist and amphibole-bearing andesite), Devonian Linong suite (sericite slate, metasandstone, and marble), and Early Carboniferous Beiwu suite (compact massive basalt, tuff, and interlayered sericite-bearing slate and marble) (Fig. 1).

2.2. Structure

The Yangla copper deposit is located between the N–S- trending Jinshajiang and Yangla faults. These faults were active beginning in Early Paleozoic, were subducted and subjected to compression during the Indosinian (Triassic Period), and were reactivated as sinistral strike-slip faults during the Himalayan Tectonic Period. Second-order faults (dipping to the NW) formed during the Himalayan, with lengths of several kilometers and widths of tens of meters. The second-order faults intersect each other, with most being thrust faults or strike-slip faults. (Gan et al., 1998; Zhan et al., 1998).

2.3. Intrusive Magmatism

In the Yangla region, a granitic intrusion is exposed in the northern Jiaren granite belt, which trends N–S in the western part of the Jinshajiang tectonic zone. Most of the granite occurs as stocks. The main granitic intrusion is the Linong granodiorite (Fig. 2), which is located in the middle of the Yangla ore district and is offset by the F4 fault, with 2 km long (N–S) and 1.5 km wide (E–W) at the surface, covering an area of 2.64 km2. Most of the intrusion is overlain by Quaternary sediment, meaning it has an irregular distribution at the surface. The wall rock is the Devonian Linong suite and the Jiangbian suite, which both occur as xenoliths in the Linong granodiorite. The granodiorite can be divided into a marginal facies (40% of the total surface area) and a center facies (60%), separated by a transition zone. The grainsize of the granodiorite varies from medium-fine to medium-coarse, and it varies in composition from intermediate at the center to acid at the margin. The granitic belt intruded the Gajinxueshan Group. Alteration of the wall rock has produced hornfels and skarn, as well as fine veins of copper mineralization and disseminated copper deposits.

The granodiorite is off-white in color, hypautomorphic and medium-coarse grained, with both compact massive and banded structure. The mineral assemblage is plagioclase (40%), K-feldspar (15%), quartz (25%), hornblende (15%), and biotite (5%), with minor zircon and apatite. The plagioclase is mainly zoned andesine, and alteration is dominated by sericitization, amphibolization, biotitization, and locally chloritization and prehnitization.

2.4. Geological characteristics of the deposit

The Yangla copper deposit is divided into five ore blocks: Jiangbian, Linong, Lunong, Jiaren, and Beiwu. The Linong ore block is the largest, and the KT2 and KT5 orebodies of the Linong ore block are the only parts of the Yangla copper deposit mined today. KT2 and KT5 is bordered by a series of gently dipping imbricate thrust faults. The orebodies dip 20°–40° to the west, although the dip increases to 50° at deeper levels (Fig. 3), and the average grade of copper in the ore is 1.03%. The hanging wall and the footwall of the orebodies consist of sandstone, marble, sericitic slate, and granodiorite. The alteration minerals include pyrite, chalcopyrite, galena, sphalerite, magnetite, limonite, and malachite. The most abundant ore minerals are chalcopyrite, pyrite, bornite, chalcosine, pyrrhotite, galena, sphalerite, and magnetite. The chalcopyrite, bornite, chalcosine are associated with Pb, Zn, Ag, Au, Bi, Sn, As, and Sb.  Oxidized ore consists of malachite, azurite, tenorite, and limonite, and gangue minerals are diopside, actinolite, garnet, quartz, calcite, mica, and feldspar. The ore show hypidiomorphic, mist-like texture, filled-sponge, striped, cracked and porphyroid textures. The ore body includes compact massive structure, disseminated structure, and fine veiny structure.

- Samples and analytical methods

We analyzed samples of ores and the Yangla granodiorite of the Yangla copper deposit. Samples of copper ore and the granodiorite were collected from the Lunong and Linong ore block in the Yangla copper deposit. The samples were analyzed for major elements, trace elements, and rare earth elements (REEs) at the Institute of Geophysics and Geochemistry Exploration, Chinese Academy of Geoscience, Langfang, China. The major elements, trace elements and REEs were analyzed by ICP–MS, for details of the analytical procedure, see Zhu et al. (2009).

The sulfur isotopic compositions of 9 sulfide samples were analyzed on a MAT 251E gas mass spectrometer by using Cu2O to oxidize the sulfides at the Geological Analysis Laboratory under the Ministry of Nuclear Industry, Beijing, China. The analytical procedure usually yielded an in-run precision of 0.2‰. The calibrations were performed with regular analyses of internal δ34S standard samples.

The lead isotopic compositions of 9 sulfide samples were analyzed on a MAT 261 mass spectrometer using the thermal ionization crosssection analytical technique at the Stable Isotope Laboratory of the Institute of Geology, Chinese Academy of Geological Sciences, Beijing, China. The precision of the 208Pb/206Pb measurements (1μg of Pb) is ≤0.005%, and the measured ratios (2σ) of international standard sample NBS981 are 208Pb/206Pb =2.16736±0.00066, 207Pb/206Pb = 207Pb/206Pb =0.91488±0.00028, and 206Pb/204Pb= 16.9386±0.0131.

Five molybdenite samples were collected from quartz and sulfide veins in the orebody of the Yangla copper deposit. The molybdenite was separated by heavy liquid separation and handpicked under a binocular microscope. 187Re and 187Os contents were measured using a TJA PQ ExCell ICP–MS housed in the Re–Os Laboratory, China Testing Center of Geology Experimentation, Beijing, China. For details of the analytical procedure, see Smoliar et al. (1996).

4.  Analytical results

4.1. Geochemical characteristics of copper ores

Table 1 lists the trace element and REE contents of copper ores from the Lunong and Linong ore blocks. The ores contain low concentrations of trace elements (∑REE=11.5 µg/g–59.2 µg/g), and the chondrite-normalized REE patterns show that LREEs slope gently to the right and HREEs are relatively flat with low concentrations (Fig. 4a). LREEs and HREEs are not obviously fractionated, with LREE/HREE = 2.1–6.3 (average, 3.4) and (La/Yb)N = 0.9–7.5. Most of the samples show a negative Ce anomaly (δCe=0.6–0.8) and possess a positive or negative Eu anomaly (δEu=0.6–1.4). Primitive-mantle-normalized trace element patterns for the copper ores (Fig. 4b) show an enrichment in large ion lithophile elements (Rb and Pb) and a strong depletion in Ba and Sr.

4.2. Geochemistry of the Yangla granodiorite

Table 2 lists the major element, trace element, and REE composition of the Linong granodiorite. The granodiorite shows little chemical variation, being characterized by high contents of Si (SiO2 = 58.3 wt.%–69.8 wt.%, with the average at 63.8 wt.%) and Al2O3 (13.4 wt.%–19.8 wt.%; average, 15.9 wt.%), low contents of Ti (TiO2 = 0.4 wt.%–0.5 wt.%; average, 0.4 wt.%) and MgO (1.5 wt.%–1.7 wt.%; average, 1.6 wt.%), and high Mg# (Mg# = Mg2+/(Mg2+ + TFe3+) × 100) (Mg# = 38–64; average, 49). The granitoids has a high alkali content (K2O+Na2O = 6.0wt.%–8.3wt.%; average, 6.8wt.%) with a ( ratio (( = [(K2O+Na2O)2]/[(SiO2 – 43)](wt.% ratio)) of 1.7–2.6 (average, 2.3).

The granodiorite is enriched in light REEs (LREEs), has a slightly negative Eu anomaly, and low contents of Y and Yb. Chondrite-normalized REE patterns show that LREEs slope to the right and that heavy REEs (HREEs) are relatively flat, with low HREE contents (Fig. 5a). The granodiorite contains medium to low REE contents (∑REE = 85.0 µg/g–119.2 µg/g; average, 104.5×10–6 µg/g), of which LREEs and HREEs are highly fractionated ((La/Yb)N = 8.9–12.4; average, 10.7; (La/Sm)N = 4.7–5.8; average, 5.3).

Primitive-mantle-normalized trace element patterns for the granodiorite (Fig. 5b) show enrichment in large ion lithophile elements (Rb, K, Pb), strong depletion in Ba, Nb, P, and Ti, and flat Dy–Lu.

  - S and Pb isotopic composition

The data listed in Table 3 show that the δ34S values of sulfides from the Yangla copper deposit vary from -9.8‰ to -0.9‰, but are mainly within the range of -4.2‰ – -0.9‰.

The data listed in Table 4 show that the sulfides are very homogeneous in their Pb isotopic composition, 208Pb/204Pb= 38.655–38.732, 207Pb/204Pb=15.703–15.735, 206Pb/204Pb=18.326–19.038.

  - Molybdenite Re–Os isotopic dating

Analyses of 5 molybdenite samples from the Yangla copper deposit are reported in Table 5. Five molybdenite samples yield model ages ranging from 229.7±3.3 to 233.0±3.4 Ma. The data, processed using the ISOPLOT/Ex program ISOPLOT 3.00 program (Ludwig, 2003), yielded a well-constrained 187Re-187Os isochron age of 233.3±3 Ma, with MSWD=0.31 and an initial 187Os of -0.77±0.93×10-9 (Fig. 6). The nearly identical model age and isochron age suggest that the analytical results are reliable.

5.  Discussion

  - Origin of ore-forming materials

Yangla copper deposit is hosted mainly by the gently dipping thrust faults near the Yangla granodiorite. Five molybdenite samples yielded a well-constrained 187Re-187Os isochron age of 233.3±3 Ma, and the Yangla granodiorite formed at 234.1±1.2 to 235.6±1.2 Ma (Indosinian) (Yang et al., 2011), the metallogenesis is therefore slightly younger than the crystallization age of the granodiorite, indicating a temporal and spatial link between the deposit and the granodiorite.

Besides the ∑REE contents, the patterns of REEs also differ between the copper ores and the granodiorite. The chondrite-normalized REE patterns of the granodiorite shows that LREEs slope to the right, with a weak negative Eu anomaly. The ores contain low REE contents, as well as LREEs and HREEs are not obviously fractionated; most of the samples possess a negative Ce anomaly and a positive or negative Eu anomaly. Comparing figure 5a with 4a reveals that the hydrothermal overprinted ore body is lower in REE, probably because the hydrothermal fluid was rich in complex REE ligands that were leached them from the rock fragments to the ore body. Europium occurred as Eu3+ dominantly at more oxidizing condition and lower temperature, resulting in the form of negative Eu anomaly. Whereas Eu3+ can be reduced to Eu2+ under reducing conditions and increased temperature, resulting in positive Eu anomaly. Eu anomaly of the copper ores in the Yangla copper deposit have a following regularity: obvious positive Eu anomaly→slightly positive Eu anomaly→obvious negative Eu anomaly from the deep ore bodies to the shallow bodies, indicating the ore-forming fluids experienced a process from reducing conditions to oxidizing conditions. Under oxidizing conditions, unlike other trivalent REE ions, Ce3+ can be readily oxidized to Ce4+, and then precipitated in the form of CeO2 or absorpted onto the surface of secondary minerals, thus the ore-forming fluids were depleted in Ce, resulting in negative Ce anomalies in the ores (Kerrich and Said, 2011).

The δ34S values of sulfides from the Yangla copper deposit vary from -9.8‰ to -0.9‰ (Fig. 7), a difference of 10.7‰. This range of isotopic values from the Yangla copper deposit indicate simultaneous incorporation of heavy and light sulfur in the hydrothermal fluids from which the ores were deposited. The most abundant ore minerals in the Yangla copper deposit are pyrrhotite, pyrite, chalcopyrite, the variation range and average of S isotopic composition from the sulfides represent S isotopic composition of the ore-forming fluids. Of the 9 sulfides analysed from the deposit, 8 have δ34S values between -4.2‰ to -0.9‰ with the average at -2.2‰, indicating a much greater contribution from the mantle to the ore-forming fluids (Harris et al., 2005; Li et al., 2006).

The data of sulfide minerals from the deposit straddle above the supracrustal lead evolution curve (Fig. 8a), and cross the orogenic evolution curve to the supracrustal lead evolution curve (Fig. 8b). The data reflects Pb mobilization from an only granulite and contributions of typical upper crustal Pb. Note that the granulites may be in an upper crustal position at the time of Pb mobilization. The Pb isotopic values of all samples from the Yangla copper deposit were calculated according to the equations Δγ = (γ − γM)×1000/γM and Δβ = (β − βM)×1000/βM (γ: 208Pb/204Pb of sample, γM: 208Pb/204Pb of mantle = 37.47, β: 207Pb/204Pb of sample, βM: 207Pb/204Pb of mantle = 15.33, Zhu, 1998),which can help in establishing the source of Pb through values of Δγ and Δβ (Fig. 9). Sulfides from the Yangla copper deposit plot in the field of the upper crust and mantle, caused by subduction-related magmatism. These results suggest that the ore-forming materials in the sulfide stage of the deposit may be derived from the Yangla granodiorite (Zhou et al., 2011).

5.2. Ore genesis

The Jinshajiang Oceanic plate was subducted to the west, beneath the Changdu-Simao block, in the late Early Permian, resulting in the formation of a series of imbricate trust faults, dipping gently to the NW, which formed in a setting of E–W compression in the Jinshajiang tectonic belt (Macpherson and Hall, 2002; Love et al., 2004).

Shallow subduction of the Jinshajiang Ocean beneath the continent interior (Burchfiel et al., 1992) resulted in a temperature gradient near the subducting plate, with the maximum temperature near the site where the subducting plate was close to the overriding plate. The subducting plate was subjected to metamorphism and partial melting, and the overriding crust was thickened by the addition of subducting plate and stacking of the upper plate (Mo et al., 2007). The resulting rise in isotherms led to partial melting of the lower crust over the subducting plate (Li et al., 2011), producing magma that ascended to the upper crust to form granite (Hezarkhani, 2006; Karsli et al., 2010). The zircon U–Pb age of the Yangla granodiorite (Yang et al., 2011), combined with its geochemical characteristics, indicates this rock is collisional, resulting from the partial melting of thickened lower crust (Wei et al., 1997). Gao et al. (2010) recognized the geochemistry of the granodiorite is in keeping with that of C-type adakites, which was triggered by westward subduction of the Jinshajiang Oceanic plate under a tectonic setting of compression.

Subduction of the Jinshajiang oceanic plate resulted in channel flow within the mantle wedge over the subducting plate (Mcinnes and Cameron, 1994; Pearce, 1995), whereby low-density material ascended and high-density material descended (Cooke et al., 2005). This circulation resulted in the accumulation of large amounts of gas–liquid fluid in the mantle wedge (Du, 2009; Wei et al., 2010), derived from the mantle and containing ore-forming material (Drummond et al., 2006; Walshe et al., 2011).

In the early Late Triassic, which was a time of transition from collision-related compression to extension in the Jinshajiang tectonic belt (Mo et al., 1993; Wang et al., 1999, 2002; Li et al., 2003), the thrust faults were E-W tensional, it would have been a favorable environment for ore-forming fluids (Kühn and Gessne, 2006). The Jinshajiang Oceanic block was subducted westward at a low angle, resulting in partial melting of the lower crust (Sajona et al., 2000), and the ascent of the magma provided a channel for the ore-forming fluid in the mantle wedge (Mungall, 2002; Luo et al., 2008). After the magma arrived at the base of the early-stage Yangla granodiorite, the platy nature of the granodiorite body would have shielded late-stage magma from the fluid. The magma would have cooled slowly, and some of the ore-forming fluid in the magma would have entered the low-angle thrust faults near the Yangla granodiorite, resulting in mineralization (Fig. 10).

6.  Conclusions

(1) S, Pb isotopic compositions of the Yangla copper deposit indicate that the ore‒forming materials were derived from the mixture of lower crust and upper mantle, also with the magmatic contributions.

(2) Five molybdenite samples yielded a well-constrained 187Re-187Os isochron age of 233.3±3 Ma, therefore, the age of metallogenesis is slightly younger than the crystallization age of the Yangla granodiorite.

(3) The Jinshajiang Oceanic block was subducted to the west, resulting in the formation of a series of gently dipping thrust faults in the Jinshajiang tectonic belt，meanwhile, accompanied magmatic activities. During a transition in geodynamic setting from collision-related compression to extension, the thrust faults were E-W tensional, it would have been a favorable environment for ore-forming fluids. The ascending magma provided a channel for the ore-forming fluid from the mantle wedge. After the magma arrived at the base of the early-stage Yangla granodiorite, the platy granodiorite at the base of the body would have shielded the late-stage magma from the fluid. The magma would have cooled slowly, and some of the ore-forming fluid in the magma would have entered the gently dipping thrust faults near the Yangla granodiorite, resulting in mineralization.

Acknowledgements

This research was jointly supported by the National Basic Research Program of China (2009CB421003, 2009CB421005) and by the 111 Project (Grant No. B07011). The authors would also like to thank two anonymous reviewers for their useful comments and constructive reviews, which significantly improved the manuscript. We would like to express our special thanks to Nelson Eby for pointing out ways of substantially improving an earlier version of this paper.

References

Burchfiel, B.C., Cowan, D.S., Davis, G.A., 1992. Tectonic overview of the Cordilleran orogen in the western United States. The Geology of North America 3, 407‒479.

Cooke, D.R., Hollings, P., Walshe, J.L., 2005. Giant porphyry deposits: Characteristics, distribution, and tectonic controls. Economic Geology 100, 801–818.

Drummond, B., Lyons, P., Goleby, B., Jones, L., 2006. Constraining models of the tectonic setting of the giant Olympic Dam iron oxide–copper–gold deposit, South Australia, using deep seismic reflection data. Tectonophysics 420, 91–103.

Du, L.T., 2009. Mantle Ichor (HACONS Fluids): The Interior Crucial Factor of Geodynamics. Acta Geoscientica Sinica 30, 739‒748 (in Chinese with English abstract).

Feng, Q.L., Ge, M.C., Xie, D.F., Ma, Z., Jiang, Y.S., 1999. Straitigraphic sequence and tectonic evolution in passive continental margin, Jinshajiang belt, northwestern Yunnan province, China. Earth Science‒Journal of China University of Geosciences 24, 553‒557 (in Chinese with English abstract).

Gan, J.M., Zhan, M.G., Yu, F.M., He, L.Q., Chen, S.F., Dong, F.L., 1998. Structural deformation and its ore-control significance in Yangla copper district, Deqin, Western Yunnan. Geology and Mineral Resources of South China 4, 59‒65 (in Chinese with English abstract).

Gao, R., Xiao, L., He, Q., Yuan, J., Ni, P.Z., Du, J.X., 2010. Geochronology, Geochemistry and Petrogenesis of Granites in Weixi-Deqin, West Yunnan. Earth Science–Journal of China University of Geosciences 35, 186–200 (in Chinese with English abstract).

Harris, A.C., Golding, S.D., White, N.C., 2005. Bajo de la Alumbrera Copper-Gold Deposit: Stable Isotope Evidence for a Porphyry-Related Hydrothermal System Dominated by Magmatic Aqueous Fluids. Economic geology 100, 863–886.

He, L.Q., Zhan, M.G., Lu, Y.F., 1998. Division of sequence stratigraphy and study on ore-bearing beds in Yangla copper orefield, western Yunnan. Geology and Mineral Resources of South China 3, 37‒41 (in Chinese with English abstract).

Hezarkhani, A., 2006. Petrology of the intrusive rocks within the Sungun Porphyry Copper Deposit, Azerbaijan, Iran. Journal of Asian Earth Sciences 27, 326–340.

Hou, Z.Q., Wang, L.Q., Zaw, K., Mo, X.X., Wang, M.J., Li, D.M., Pan, G.T., 2003. Postcollisional crustal extension setting and VHMS mineralization in the Jinshajiang orogenic belt, southwestern China. Ore Geology Reviews 22, 177–199.

Hu, G.L., Jiang, H., Jiang. J., Hu, D.P., Niu, C.L., 2008. An analysis of the ore-controlling factors of Deqin Yangla copper ore district in Yunnan and its ore-hunting prospect. Metal Mine 28, 87‒89 (in Chinese with English Abstract).

Jian, P., Liu, D.Y., Kröner, A., Zhang, Q., Wang, Y.Z., Sun, X.M., Zhang, W., 2009. Devonian to Permian plate tectonic cycle of the Paleo-Tethys Orogen in southwest China (II): Insights from zircon ages of ophiolites, arc/back-arc

assemblages and within-plate igneous rocks and generation of the Emeishan CFB province. Lithos 113, 763–784.

Karsli, O., Dokuz, A., Uysal, I., Aydin, F., Kandemir, R.,Wijbrans, J., 2010. Generation of the Early Cenozoic adakitic volcanism by partial melting of mafic lower crust, Eastern Turkey: Implications for crustal thickening to delamination. Lithos 114, 109–120.

Kerrich, R., Said, N., 2011. Extreme positive Ce-anomalies in a 3.0 Ga submarine volcanic sequence, Murchison

Province: Oxygenated marine bottom waters. Chemical Geology 280, 232–241.

Kühn, M., Gessner, K., 2006. Reactive transport model of silicification at the Mount Isa copper deposit, Australia. Journal of Geochemical Exploration 89, 195–198.

Li, J.X., Qin, K.Z., Li, G.M., Bo, X., Lei, C., Zhao, J.X., 2011. Post-collisional ore-bearing adakitic porphyries from Gangdese porphyry copper belt, southern Tibet: Melting of thickened juvenile arc lower crust. Lithos 126, 265–277.

Li, S.L., Su, C.X., Yan, Y.F., Ning, X.F., 2008. Research on geological features and mineragenesis laws of Yagra copper deposit. Express Information of Mining Industry 12, 27‒30 (in Chinese with English Abstract).

Li, X.B., Huang, Z.L., Li, W.B., Zhang, Z.L., Yan, Z.F., 2006. Sulfur isotopic compositions of the Huize super-large Pb–Zn deposit, Yunnan Province, China: Implications for the source of sulfur in the ore-forming fluids. Journal of Geochemical Exploration 89, 227‒230.

Li, Y., Wang, C.S., Yi, H.S., 2003. The Late Triassic collision and sedimentary responses at western segment of Jinshajiang suture, Tibet. Acta Sedmentologica Sinica 21, 191‒197 (in Chinese with English abstract).

Lin, S.L., Wang, L.Q., 2004. Structural features of the Yagra copper deposit in Deqen, Yunnan. Sedimentary Geology and Tethyan Geology 24, 48-51.

Liu, X.L., Zhang, N., Yin, G.H., Wang, C.W., Luo, H.Y., 2009. Beiwu-Nilu Cu deposit of Yangla, Deqin, Yunnan. Yunnan Geology 28, 34‒39 (in Chinese with English Abstract).

Love, D.A., Clark, A.H., Glover, J.K., 2004. The Lithologic, Stratigraphic, and Structural Setting of the Giant Antamina Copper-Zinc Skarn Deposit, Ancash, Peru. Economic Geology 99, 887‒916.

Lu, Y.F., Chen, K.X., Zhan, M.G., 1999. Geochemical evidence of exhalative-sedimentary ore-bearing skarns in Yangla copper mineralization concentrated area, Deqin county, northwestern Yunnan province. Earth Science−Journal China University of Geoscience 21, 191‒197 (in Chinese with English abstract).

Ludwing, K.R., 2003. ISOPLOT 3.00: A Geochronological toolkit for Microsoft Excel. Berkeley Geochronology Center Special Publication, pp. 1–70.

Luo, Z.H., Lu X.X., Guo, S.F., 2008. Metallogenic systems on the transmagmatic fluids theory. Acta Petrologica Sinica 24, 2669‒2678 (in Chinese with English abstract).

Macpherson, C.G., Hall, R., 2002. Timing and tectonic controls in the evolving orogen of SE Asia and the western Pacific and some implications for ore generation. Geological Society, London, Special Publications 204, 49–67.

Mcinnes, B.I.A., Cameron, E.M., 1994. Carbonated, alkaline hybridizing melts from a subarc environment–mantle wedge samples from the Tabar-Lihir Tanga-Feni Arc, Papua-New-Guinea. Earth and Planetary Science Letters 122, 125–141.

Metcalfe, I., 2002. Permian tectonic framework and paleogeography of SE Asia. Journal of Asian Earth Sciences 20, 551–566.

Mo, X.X., Lu, F.X., Shen, S.Y., 1993. San Jiang tethyan volcanism and related mineralization. Geological Publishing House, Beijing, pp. 1–266 (in Chinese with English abstract).

Mo, X.X., Hou, Z.Q., Niu, Y.L., Dong, G.C., Qu, X.M., Zhao, Z.D., Yang, Z.M., 2007. Mantle contributions to crustal thickening during continental collision: Evidence from Cenozoic igneous rocks in southern Tibet. Lithos 96, 225–242.

Mungall, J.E., 2002. Roasting the mantle; slab melting and the genesis of major Au and Au-rich Cu deposits. Geology 30, 915–918.

Pan, G.T., Xu, Q., Hou, Z.Q., Wang, L.Q., Du, D.X., Mo, X.X., 2003. Archipelagic orogenesis, metallogenic systems and assessment of the mineral resources along the Nujiang-Lancangjiang-Jinshajiang area in southwestern China. Geological Publishing House, Beijing, pp. 171‒192 (in Chinese with English Abstract).

Pan, J.Y., Zhang, Q., Li, C.Y., 2000. REE geochemistry of the Yangla copper deposit in western Yunnan. Acta Mineralogical Sinica 20, 44‒49.

Pan, J.Y., Zhang, Q., Ma, D.S., 2001. Cherts from the Yangla copper deposit, western Yunnan province: Geochemical characteristics and relationship with massive sulfide mineralization. Science in China (D) 44, 237‒244.

Pearce, J.A., 1995. Tectonic implications of the composition of volcanic arc magmas. Annual Review of Earth and Planetary Sciences 23, 251‒285.

Qu, X.M., Yang, Y.Q., Li, Y.G., 2004. A discussion on origin of Yangla copper deposit in light of diversity of ore‒hosting rock types. Mineral Deposits 23, 431‒442 (in Chinese with English abstract).

Sajona, F.G., Maury, R.C., Pubellier, M., Leterrier, J., Bellon, H., Cotten, J., 2000. Magmatic source enrichment by slab-derived melts in a young post-collision setting, central Mindanao (Philippines). Lithos 54, 173–206.

Smoliar, M.L., Walker, R.J., Morgan, J.W., 1996. Re-Os ages of group ⅠA, ⅡA, ⅣA and ⅣB iron meteorites. Science 271, 1099–1102.

Sun, S.S., McDonough, W.F., 1989. Chemical and isotopic systematics of oceanic basalts: Implication for the mantle composition and process. In: Magmatism in Ocean Basins (A.D. Saunders & M.J. Norry, eds.). Geological Society of London Special Publication 42, 313–345.

Walshe, J.L., Solomon, M., Whitford, D.J., Sun, S.S., Foden, J.D., 2011. The role of the mantle in genesis of tin deposits and tin provinces of eastern Australia. Economic Geology 106, 297‒305.

Wang, L.Q., Pan, G.T., Li, D.M., Xu, Q., Lin, S.L., 1999. The spatio-temporal framework and geological evolution of the Jinshajiang arc-basin systems. Acta Geologica Sinica 73, 206‒218 (in Chinese with English abstract).

Wang, X.F., Metcalfe, I., Jian, P., He, L.Q., Wang, C.S., 2000. The Jinshajiang–Ailaoshan suture zone, China: Tectonostratigraphy, age and evolution. Journal of Asian Earth Sciences 18, 675–690.

Wang, L.Q., Hou, Z.Q., Mo, X.X, Wang, M.J., Xu, Q., 2002. The post-collisional crustal extension setting: an Important mineralizing environment of volcanic massive sulfide deposits in Jinshajiang orogenic belt. Acta Geologica Sinica 76, 541‒556 (in Chinese with English abstract).

Wei, J.Q., Zhan, M.G., Lu, Y.F., Chen, K.X., He, L.Q., 1997. Geochemistry of granitoids in Yangla ore district, western Yunnan. Geology and Mineral Resources of south China 50‒56 (in Chinese with English abstract).

Wei, J.Q., Chen, K.X., He, L.Q., 1999. A discussion on the structural environment for forming the volcanic rock in Yangla region. Yunnan geology 18, 53‒62 (in Chinese with English Abstract).

Wei, J.Q., Chen, K.X., Wei, F.Y., 2000. Tectonism-magmatism-mineralization in Yangla region, western Yunnan. Geology and Mineral Resources of South China 1, 59‒62 (in Chinese with English abstract).

Wei, W.B., Jin, S., Ye, G.F., 2010. Conductivity structure and rheological property of lithosphere in Southern Tibet inferred from super-broadband magnetotelluric sounding. Science in China (D) 53, 189‒202.

Xiao, L., Qi, H., Pirajno, F., Ni, P.Z., Du, J.X., Wei, Q.R., 2008. Possible correlation between a mantle plume and the evolution of Paleo-Tethys Jinshajiang Ocean: Evidence from a volcanic rifted margin in the Xiaru-Tuoding area, Yunnan, SW China. Lithos 100, 112–126.

Yang, G.Q., 2009. Geological characteristics, genesis and metallogenic prediction of the Yangla copper deposit in Deqin, Yunnan province, China. Ph.D. thesis, China University of Geosciences, Beijing (in Chinese with English abstract).

Yang, X.A., Liu, J.J., Han, S.Y., Zhang, H.Y., Luo, C., Wang, H., Chen, S.Y., 2011. U-Pb dating of zircon from the Linong granodiorite, Re-Os dating of molybdenite from the ore body and their geological significances in Yangla copper deposit, Yunnan. Acta Petrologica Sinica 27, 2567–2576 (in Chinese with English abstract).

Zartman, R.E., Doe, B.R., 1981. Plumbotectonics the model. Tectonophysics 75, 135‒162.

Zhan, M.G., Lu, Y.F., Chen, S.F., Dong, F.L., Chen, K.X., Wei, J.Q., He, L.Q., Huo, X.S., 1998. Yangla copper deposit in Deqin, western China. China University of Geoscience Publishing House, Wuhan, pp. 30‒44 (in Chinese).

Zhou, T.F., Wu, M.G., Fan, Y., Duan, C., Yuan, F., Zhang, L.J., Liu, J., Qian, B., Franco, P., David, R.C., 2011. Geological, geochemical characteristics and isotope systematics of the Longqiao iron deposit in the Lu-Zong volcano-sedimentary basin, Middle-Lower Yangtze (Changjiang) River Valley, Eastern China. Ore Geology Reviews 43, 154–169.

Zhu, B.Q., 1998. The theory and application of the isotopic systematic in Geoscience-concurrent discussion of the continental crust and mantle evolvement in China. Science Publishing House, Beijing, pp. 1‒330 (in Chinese with English abstract).

Zhu, J., Zeng, P.S., Zeng, L.C., Yin, J., 2009. Stratigraphic subdivision of the Yangla copper ore district, northwestern Yunnan. Acta Geologica Sinica 83, 1415‒1420 (in Chinese with English abstract).

Zhu, J.J., Hu, R.Z., Bi, X.W., Zhong, H., Chen, H., 2011. Zircon U–Pb ages, Hf–O isotopes and whole-rock Sr–Nd–Pb isotopic geochemistry of granitoids in the Jinshajiang suture zone, SW China: Constraints on petrogenesis and tectonic evolution of the Paleo-Tethys Ocean. Lithos 126, 248–264.

Zhu, L.M., Zhang, G.W., Li, B., Guo, B., Kang, L., Lv, S.L., 2009. Geology, isotope geochemistry and ore genesis of the Maanqiao gold deposit, Shanxi province. Acta Petrologica Sinica 25, 431‒443.

Fig. 1.  Geological map of the Yangla copper deposit (after Qu et al., 2004) .

1. Paleogene; 2. Upper Triassic; 3. Lower Triassic; 4. Upper Permian; 5. Lower Permian; 6. Gajinxueshan group; 7. Ultrabasic rock; 8. Carboniferous; 9. Devonian; 10. Silurian; 11. Ordovician; 12. Proterozoic; 13. Quartzdiorite; 14. Granitoids; 15. Copper deposit; 16. Fault; 17. Geological boundary; 18. Yangla mineral district; 19. Region of interest; Ⅰ. Yangtze block; Ⅱ. Ganzi-Litang melange belt; Ⅲ. Yidun arc belt; Ⅳ. Zhongza-Zhongdian block; Ⅴ. Jinshajiang melange belt; Ⅵ. Jiangda-Weixi arc belt; Ⅶ. Changdu-Simao block; Ⅷ. Lancangjiang melange belt; Ⅸ. Chayu block; Ⅹ. Tuoba-Yanjing arc belt; Ⅺ. Nujiang melange belt.

Fig. 2.  Geological sketch map of the Yangla copper deposit (after Yang, 2009).

1. Quaternary slope material; 2. Beiwu suite: massive basalt interlayered with sericite slate and marble; 3. Linong suite: sericite slate, metasandstone, and marble; 4. Jiangbian suite: marble, sericite slate, and metasandstone; 5. Plagiogranite; 6.  Granodiorite; 7. Ore body and corresponding number; 8. Boundary between alteration zones; 9. Sericite-chlorite alteration zone; 10. Hornfels alteration zone; 11. Skarnization alteration zone; 12. Quartz–sericite alteration zone; 13. Chlorite–epidote alteration zone; 14. K-feldspar–quartz alteration zone; 15. Sericite–calcite alteration zone.

Fig. 3.  No.13 prospecting line profile map in the Linong ore block of the Yangla copper deposit (after Yang, 2009).

1. Explosive breccia; 2. Metasandstone; 3. Marble; 4. Granodiorite; 5. Drilling and numbers; 6. Tunnel and numbers

Fig. 4.  Chondrite-normalized REE patterns (a) and primitive-mantle-normalized trace element patterns (b) for copper ores of the Yangla copper deposit.

Fig. 5.  Chondrite-normalized REE patterns (a) and primitive-mantle-normalized trace element patterns (b) for the Linong granodiorite (chondrite and primitive mantle data are from Sun and McDonough, 1989).

Fig. 6.  Re–Os isochron diagrams for the molybdenite samples from the Yangla copper deposit

Fig. 7.  Composite sulfur isotopic composition histogram of the Yangla copper deposit.

Fig. 8.  Lead isotope compositions (207Pb/204Pb versus 206Pb/204Pb and 208Pb/204Pb versus 206Pb/204Pb) of samples from the Yangla copper deposit plotted in the model lead evolution diagrams of Zartman and Doe(1981).

M. mantle-source lead; O. orogenic belt-source lead; U. supracrust-source lead; L. lower crust-source lead.

Fig. 9.  Δγ-Δβ diagram of ore lead from the Yangla copper deposit (after Zhu, 1998).

Fig. 10.  Schematic cross-section through the Yangla copper deposit (modified from Pearce, 1995).

1. Crust; 2. Mantle lithosphere; 3. Mantle asthenosphere; 4. Plate motion; 5. Mantle fluid advection.